ClarkDietrich® Exterior Framing

Section 070543 Cladding Support Systems

- GENERAL

        - DELIVERY, STORAGE, AND HANDLING

        - Protect cold-formed metal framing from corrosion, deformation, and other damage during delivery, storage, and handling as required by AISI S202.

- PRODUCTS

      - PERFORMANCE REQUIREMENTS

        - Cold-Formed Steel Framing Standards: Unless more stringent requirements are indicated, framing to comply with AISI S100 and AISI S240.

        - Design wall systems in consideration of thermal expansion and contraction effects. Include thermal breaks in accordance with pertinent codes and regulations of Authorities Having Jurisdiction.

      - CONTINUOUS INSULATION RAINSCREEN FRAMING SYSTEM

        - Framing Members, General: Comply with AISI S240 for conditions indicated.

        - Steel Sheet: ASTM A1003/A1003M, Structural Grade, Type H, metallic coated, of grade and coating designation as follows:

          - Grade: ST50H (ST340H).

          - Coating: [CP 90: G90 (Z275), AZ50 (AZM150), or GF45 (ZGF135)] [CP 90: G90 (Z275), AZ50 (AZM150), or GF45 (ZGF135) with black powder coating].

        - Vented Rainscreen Attachment System: Hat-shaped channel for exterior wall cladding, with pre-punched holes for fastening and vent holes for moisture drainage and air movement. Channel is attached over mineral wool insulation using manufacturer’s tested thermally-isolated fasteners.

          - Product: ClarkDietrich; ProChannel Ci Cladding Support with Grip-Deck TubeSeal® Technology.

          - Minimum Base-Steel Thickness: 0.0538 inch (1.37 mm).

          - Channel Depth: 7/8 inch (22 mm).

          - Orientation: [Horizontal] [Vertical].

      - ACCESSORIES

        - Mechanical Fasteners:

          - Comply with ASTM C 1513; manufacturer’s recommended thermally-isolated self-tapping, steel drill fasteners with integral sleeve, for fastening vented rainscreen attachment system to [cold-formed steel] [wood] structural framing.

            - Fastener Depth: Coordinate fastener depth with thickness of insulation required.

- EXECUTION

      - EXAMINATION

        - Examine substrates, areas, conditions, and abutting structural framing for compliance with requirements for installation tolerances and other conditions affecting performance of the Work.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - PREPARATION

        - Ensure air/water barrier is fully installed and cured in accordance with manufacturer’s instructions and Project requirements.

        - Flash and seal all fenestration, transitions, discontinuities, sills, and ledgers in accordance with manufacturer’s instructions and project requirements.

        - Refer to manufacturer’s structural span tables for recommended channel and fastener spacing.

      - INSTALLATION OF VENTED RAINSCREEN ATTACHMENT SYSTEM

        - Install vented rainscreen attachment system over studs and continuous mineral wool insulation, in accordance with ASTM C1007, AISI S240, and manufacturer’s written instructions, unless more stringent requirements are indicated.

        - Fasten channels through insulation and sheathing, into structural studs using manufacturer’s recommended thermally-isolated fasteners.

        - Install manufacturer’s recommended thermally-isolated fasteners in accordance with system manufacturer’s installation guidelines.

          - Comply with requirements for spacing, edge distances, and minimum penetration depth.